PRODUCT:-  WATER BASED RADIATOR ENAMEL

REFERENCE:-  Q/122/1

COLOUR:-  WHITE

FINISH:-  MID GLOSS

TYPE:-  ACRYLIC POLYMER, WATER

THINNABLE

TYPICAL SG:-  1.2 AT 20(C

TYPICAL VISCOSITY:-  2.5 POISE AT 25(C

(ICI CONE AND PLATE)

TYPICAL  SOLIDS:-  36% BY VOLUME

FLASH POINT:-  NON-FLAMMABLE

RECOMMENDED THINNERS:-  CLEAN WATER

APPLICATION:-  BRUSH OR ROLLER

(DO NOT APPLY WHEN THE

TEMPERATURE IS BELOW 5(c)

After each application allow to dry for one hour, then stove with the radiator at full heat (70(C) for one hour to ensure drying.

*COVERAGE GUIDE:-  13m2/litre

*DRYING TIME:-  SURFACE DRY -  1   HOUR

THROUGH DRY  - 2 HOURS - (see

application notes)

COLD DAMP CONDITIONS WILL

PROLONG THESE TIMES

OVERCOAT TIME MIN 3 HOURS

STORAGE:-  PROTECT FROM FROST AND

ABNORMAL HEAT

USES:-  AS A HIGH PERFORMANCE

WATERBASED RADIATOR

ENAMEL DESIGNED FOR

APPLICATION TO DOMESTIC HOT

WATER RADIATORS.

VOC:-  BELOW 100	g/litre

HEALTH & SAFETY:-  SEE SDS 10676

*BY BRUSH TO A DRIED FILM THICKNESS OF 25 MICRONS AT 20oC.