PRODUCT:-  GLASS SHADING

REFERENCE:-  W/454/1

COLOUR:-  WHITE

FINISH:-  MATT

TYPE:-  AQUEOUS MIXED POLYMER

DISPERSION

TYPICAL SG:-  1.68 AT 20C

TYPICAL VISCOSITY:-  PASTE

TYPICAL TOTAL SOLIDS:-  70%

FLASH POINT:- NON-FLAMMABLE

RECOMMENDED THINNERS:-  WATER

APPLICATION:-  BRUSH OR ROLLER.  DILUTE 							BEFORE USE AS REQUIRED

E.G. 2 PARTS PASTE:1PART                        						WATER.

DO NOT APPLY WHEN THE

TEMPERATURE IS BELOW 5C

*COVERAGE GUIDE:-  DEPENDANT ON DILUTION

GUIDE:20 m2 /l @ 2:1 DILUTION AS  						ABOVE

*DRYING TIME:-  1-2 HOURS.  COLD, DAMP

CONDITIONS WILL PROLONG

THE TIME.

STORAGE:-   PROTECT FROM FROST AND

ABNORMAL HEAT.

HEALTH & SAFETY DATA:-  SEE SDS 10628

*BY BRUSH TO A DRIED FILM THICKNESS OF 10-20 MICRONS AT 20oC.