PRODUCT:-  HAMMERCOTE SMOOTH SATIN

REFERENCE:-  G126/2

COLOUR:-  BLACK

FINISH:-  SATIN

TYPE:-  MODIFIED ALKYD

TYPICAL SG:-  1.14@ 20(C

TYPICAL VISCOSITY:-  8.0 – 10.0  POISE @ 25(C

TYPICAL TOTAL SOLIDS:-  59% BY WEIGHT

46% BY VOLUME

FLASH POINT:-  23(C

RECOMMENDED THINNERS:-  V/607/15 FOR BRUSH USE,

CLEANING ETC.

V/607/16 FOR SPRAYING (10%

ADDITION AS START GUIDE,

AMOUNT NECESSARY BEING

DEPENDANT UPON TYPE OF

EQUIPMENT AND USER)

APPLICATION:-  BY BRUSH OR SPRAY

*COVERAGE GUIDE:-  10 SQ. METRES/LITRE

*DRYING TIME:-  SURFACE DRY - ½ HOUR

THROUGH DRY - 6 HOURS

USES:-  AS A FAST DRYING FINISH

GIVING A HARD DURABLE FILM.

THE USE OF A PRIMER

ENHANCES ADHESION TO METAL

THE RECOMMENDED TYPE IS

WATER BASED ALL METALS PRIMER

HEALTH & SAFETY:-  SEE SDS 11315

*BY BRUSH TO A DRIED FILM THICKNESS OF 40 - 45 MICRONS AT 20oC.