PRODUCT:-  WATER BASED RADIATOR ENAMEL

REFERENCE:-  Q/122/1

COLOUR:-  WHITE

FINISH:-  MID GLOSS

TYPE:-  ACRYLIC POLYMER, WATER

THINNABLE

TYPICAL SG:-  1.2 AT 20C

TYPICAL VISCOSITY:-  2.5 POISE AT 25C

(ICI CONE AND PLATE)

TYPICAL  SOLIDS:-  36% BY VOLUME

FLASH POINT:-  NON-FLAMMABLE

RECOMMENDED THINNERS:-  CLEAN WATER

APPLICATION:-  BRUSH OR ROLLER

(DO NOT APPLY WHEN THE

TEMPERATURE IS BELOW 5c)

After each application allow to dry for one hour, then stove with the radiator at full heat (70C) for one hour to ensure drying.

*COVERAGE GUIDE:-  13m2/litre

*DRYING TIME:-  SURFACE DRY -  1   HOUR

THROUGH DRY  - 2 HOURS - (see

application notes)

COLD DAMP CONDITIONS WILL

PROLONG THESE TIMES

OVERCOAT TIME MIN 3 HOURS

STORAGE:-  PROTECT FROM FROST AND

ABNORMAL HEAT

USES:-  AS A HIGH PERFORMANCE

WATERBASED RADIATOR

ENAMEL DESIGNED FOR

APPLICATION TO DOMESTIC HOT

WATER RADIATORS.

VOC:-  BELOW 100	g/litre

HEALTH & SAFETY:-  SEE SDS 10676

*BY BRUSH TO A DRIED FILM THICKNESS OF 25 MICRONS AT 20oC.